3.1 Experimental result

The measured DC resistance Rmean, effective electrical conductivity σeff, and the associated standard deviations RSD and σSD obtained for the three lattice architectures (n = 3 specimens per architecture) are listed in Table 2. The specimen geometry parameters—gauge length L and cross-sectional area A—are included for reference.

Table 2. DC resistance and effective electrical conductivity of sintered Graphene/SiC lattices (n = 3 per architecture).

| Lattice Structure | 𝑳 (mm) | 𝑨 (mm²) | Rmean (Ω) | RSD (Ω) | σeff (S/m) | σSD (S/m) |
| --- | --- | --- | --- | --- | --- | --- |
| Grid | 14.06 | 64.402 | 34.983 | 0.532 | 6.240 | 0.095 |
| Scaffold | 14.25 | 66.07 | 21.75 | 0.690 | 9.916 | 0.314 |
| Honeycomb | 14.28 | 63.536 | 20.676 | 0.477 | 10.869 | 0.250 |

The Grid architecture yielded the highest mean resistance (Rmean = 34.983 ± 0.532 Ω) and the lowest effective conductivity (σeff = 6.240 ± 0.095 S/m). The Scaffold architecture showed intermediate values: Rmean = 21.75 ± 0.690 Ω and σeff = 9.916 ± 0.314 S/m. The Honeycomb architecture exhibited the lowest resistance (Rmean = 20.676 ± 0.477 Ω) and the highest effective conductivity (σeff = 10.869 ± 0.250 S/m). Accordingly, Rmean decreases monotonically in the order Grid > Scaffold > Honeycomb, while σeff increases in the reverse order: Grid < Scaffold < Honeycomb. These trends are illustrated graphically in Fig. 10, which plots Rmean (Fig. 10(a)) and σeff (Fig. 10(b)) as a function of lattice architecture. The error bars represent the standard deviation of three independently printed and sintered specimens.

Fig. 10. Experimentally measured (a) mean DC resistance Rmean (Ω) and (b) effective electrical conductivity σeff (S/m) as a function of lattice architecture (Grid, Honeycomb, Scaffold). Error bars represent standard deviation (n = 3).