FEA Analysis and Experiment with Different 3D Graphene/SiC Structures

# 1. Introduction

Silicon carbide (SiC) is among the most widely studied advanced structural ceramics, combining high hardness, low density, excellent thermal stability, chemical inertness, and competitive electrical properties that make it indispensable in aerospace propulsion, high-temperature structural components, semiconductor processing equipment, and functional electrodes.? The rapid expansion of additive manufacturing (AM) has opened new pathways for fabricating SiC-based components with complex internal geometries inaccessible by conventional powder-pressing or machining routes,? yet the intrinsic brittleness of monolithic SiC and its limited electrical conductivity — which restricts its use in structural electrodes, resistive heaters, and electromagnetic interference shielding — continue to motivate research into composite reinforcement strategies that simultaneously broaden mechanical reliability and functional performance.

Graphene, first isolated in 2004,? possesses a theoretical Young’s modulus of ~1 TPa, in-plane thermal conductivity exceeding 3000 W·m⁻¹·K⁻¹, and outstanding electron mobility. Incorporating graphene-related materials (GRMs), principally graphene nanoplatelets (GNPs), into ceramic matrices simultaneously improves fracture toughness through crack deflection and bridging while establishing percolated conductive networks.? In the SiC matrix, GNP additions raise room-temperature electrical conductivity by up to three orders of magnitude, reaching ~4380 S·m⁻¹ at 20 vol.% GNP in dense bulk specimens consolidated by spark plasma sintering (SPS) — roughly twice the value measured for a robocast filament of equivalent composition, owing to the ~43 vol.% porosity of the extruded rod.? This intrinsic sensitivity to porosity and microstructure implies that, in DIW-fabricated lattices, macroscopic effective conductivity is governed not only by material composition but also by the architectural parameters of the printed structure.

Direct Ink Writing (DIW, or robocasting) enables layer-by-layer extrusion of viscoelastic pastes through a calibrated nozzle along computer-programmed toolpaths, producing three-dimensional lattice structures with parametrically defined topology at room temperature and without high-energy radiation sources.? The technique accommodates a broad spectrum of ceramic systems — including alumina, SiC, zirconia, silicon nitride, and ultra-high-temperature ceramics — with solid loadings up to and exceeding 40 vol.%,? and standardisation efforts alongside ink formulation meta-analyses have established empirical printability criteria correlating yield stress and viscosity with successful filament deposition.?

DIW-fabricated graphene/SiC composites have demonstrated the potential to combine geometric design freedom with superior electrical performance. Román-Manso et al. reported robocast graphene/SiC scaffolds sintered by SPS with effective conductivities up to 611 S·m⁻¹ and measurable filament-orientation anisotropy,? while PCS-based DIW inks have enabled graphene/SiCp/SiC lattices with density as low as 1.08 g·cm⁻³ and conductivity of 670 S·m⁻¹.? Beyond DIW, vat photopolymerisation of SiC ceramics incorporating graphene percolation networks has yielded conductivities up to 1000 S·m⁻¹ alongside low thermal conductivity (62–88 mW·m⁻¹·K⁻¹), confirming the broader potential of 3D-printed conductive SiC for high-temperature electronics.? In the alumina/GNP system, DIW-printed scaffolds confirm that graphene addition simultaneously boosts compressive strength by up to 80% and quadruples thermal conductivity relative to plain alumina at equivalent porosity, highlighting the multifunctional potential of GRM-reinforced 3D-printed ceramic lattices.?

Building on these experimental results, finite element analysis has become essential for rationalising transport in porous ceramic lattices, where complex internal geometry precludes simple analytical estimates. FEM elastic simulations of robocast alumina/GNP scaffolds validated against Impulse Excitation Technique and Resonant Ultrasound Spectroscopy confirmed that FEM accurately captures lattice anisotropy arising from the print pattern and coaxial strut configuration.? FEM of coaxially printed ceramic scaffolds for thermal energy storage further showed that the multi-layered filament architecture controls anisotropic thermal response and enables simultaneous optimisation of energy storage density and thermal conductivity.? For highly porous composites (porosity >55%), Monte Carlo equivalent-circuit models reproduce effective electrical conductivity from minimal input parameters and extract microstructural information otherwise inaccessible experimentally.? Systematic four-probe characterisation of extrusion-printed graphene structures confirms that macroscopic conductivity depends not only on percolation and graphene content but also on inter-filament contact quality and printing architecture,? establishing lattice topology as an independent design variable for electrical transport. Initial FEM modelling of robocast graphene/SiC scaffolds reproduced the conductivity trend with GNP fraction and identified interlayer contact geometry and current-path tortuosity as the primary architectural parameters governing macroscopic σeff.?

PCS-derived DIW systems are particularly well-suited for topology-dependent conductivity studies because pyrolytic conversion preserves the designed macroporous topology while yielding electrically continuous SiC composite struts, enabling independent variation of strut composition and lattice architecture.? The maturity of the broader DIW/SiC composite platform has been demonstrated across a range of material systems,? yet topology-dependent electrical conductivity and its quantitative FEM prediction remain unaddressed.

Despite this body of work, three key questions remain open. First, no study has systematically compared how different in-plane filament arrangements — orthogonal cross-ply (Scaffold), diamond-pattern meander (Grid), and hexagonal zig-zag (Honeycomb) — affect the effective electrical conductivity of DIW-printed graphene/SiC lattices at constant composition and comparable solid volume. Second, DC conduction FEM simulations of topology-controlled graphene/SiC lattices with experimentally calibrated intrinsic strut conductivity have not been reported, leaving the separate contributions of interlayer contact area, filament–field alignment, and current-path tortuosity to macroscopic σeff unresolved. Third, the architecture-dependent dissipation mechanisms — whether dominated by contact resistance at filament junctions, current-path tortuosity, or field misalignment — that cause systematic offsets between FEM predictions and measured conductivity in DIW-fabricated graphene/SiC lattices have not been identified.

The present work addresses these gaps. Three topology-controlled graphene/SiC lattice architectures — Scaffold, Grid, and Honeycomb — were designed with identical filament diameter and comparable solid volumes, fabricated by DIW from a PCS-based graphene/SiC paste, and sintered at 1300°C via preceramic polymer pyrolysis. Effective electrical conductivity was evaluated by: (i) steady-state DC conduction FEM in ANSYS Maxwell 3D, using the intrinsic conductivity of the composite measured by four-wire DC characterisation of calibration filaments from the same feedstock; and (ii) four-probe DC resistance measurements on three independently fabricated specimens per architecture. The topology-dependent current-density vector (J-vector) distributions from FEM are analysed to identify the structural origins of the conductivity ranking — with emphasis on interlayer contact area Aint, filament orientation relative to the electric field, and local current-path tortuosity — and the FEM–experiment agreement is assessed to identify architecture-dependent dissipation mechanisms.

# References

[1]  N.P. Padture, Advanced structural ceramics in aerospace propulsion, Nat. Mater. 15 (2016) 804–809. https://doi.org/10.1038/nmat4687

[2]  Y. Lakhdar, C. Tuck, J. Binner, A. Terry, R. Goodridge, Additive manufacturing of advanced ceramic materials, Prog. Mater. Sci. 116 (2021) 100736. https://doi.org/10.1016/j.pmatsci.2020.100736

[3]  L. Duan, M. Bai, N. Xiao, L. Zhang, H. Wang, Y. Wu, B. Dong, W. Tang, Y. Li, Z. Zhang, W. Ming, A review of recent advances in ceramic 3D printing technologies, J. Manuf. Process. 157 (2026) 1091–1122. https://doi.org/10.1016/j.jmapro.2025.12.057

[4]  K.S. Novoselov, A.K. Geim, S.V. Morozov, D. Jiang, Y. Zhang, S.V. Dubonos, I.V. Grigorieva, A.A. Firsov, Electric Field Effect in Atomically Thin Carbon Films, Science 306 (2004) 666–669. https://doi.org/10.1126/science.1102896

[5]  C. Ramírez, M. Belmonte, P. Miranzo, M.I. Osendi, Applications of Ceramic/Graphene Composites and Hybrids, Materials 14 (2021) 2071. https://doi.org/10.3390/ma14082071

[6]  P. Miranzo, M. Belmonte, M.I. Osendi, From bulk to cellular structures: A review on ceramic/graphene filler composites, J. Eur. Ceram. Soc. 37 (2017) 3649–3672. https://doi.org/10.1016/j.jeurceramsoc.2017.03.016

[7]  N. Khobragade, Graphene reinforced SiC ceramic composites using powder metallurgy route: A short review, Mater. Today Proc. 16 (2024) 3617–3635. https://doi.org/10.1016/j.matpr.2024.05.128

[8]  A. Almansoori, K. Balázsi, C. Balázsi, Advances, Challenges, and Applications of Graphene and Carbon Nanotube-Reinforced Engineering Ceramics, Nanomaterials 14 (2024) 1881. https://doi.org/10.3390/nano14231881

[9]  B. Román-Manso, E. Domingues, F.M. Figueiredo, M. Belmonte, P. Miranzo, Enhanced electrical conductivity of silicon carbide ceramics by addition of graphene nanoplatelets, J. Eur. Ceram. Soc. 35 (2015) 2723–2731. https://doi.org/10.1016/j.jeurceramsoc.2015.03.044

[10] J.A. Lewis, Direct Ink Writing of 3D Functional Materials, Adv. Funct. Mater. 16 (2006) 2193–2204. https://doi.org/10.1002/adfm.200600434

[11] A. Shahzad, I. Lazoglu, Direct ink writing (DIW) of structural and functional ceramics: Recent achievements and future challenges, Compos. Part B Eng. 225 (2021) 109249. https://doi.org/10.1016/j.compositesb.2021.109249

[12] E.F. Cárdenas Correa, E.A. Torres Barahona, J.B. Carda Castelló, Additive Manufacturing of Ceramic Materials via Direct Ink Writing (DIW): A Review, Ceramics 9 (2026) 16. https://doi.org/10.3390/ceramics9020016

[13] E. Feilden, E.G.-T. Blanca, F. Giuliani, E. Saiz, L. Vandeperre, Robocasting of structural ceramic parts with hydrogel inks, J. Eur. Ceram. Soc. 36 (2016) 2525–2533. https://doi.org/10.1016/j.jeurceramsoc.2016.03.001

[14] A.J. Allen, I. Levin, R.A. Maier, Research, standards, and data needs for industrialization of ceramic direct ink writing, Int. J. Ceram. Eng. Sci. 4 (2022) 302–308. https://doi.org/10.1002/ces2.10158

[15] Z.L. Li, S. Zhou, E. Saiz, R. Malik, Ink formulation in direct ink writing of ceramics: A meta-analysis, J. Eur. Ceram. Soc. 44 (2024) 6777–6796. https://doi.org/10.1016/j.jeurceramsoc.2024.05.014

[16] B. Román-Manso, F.M. Figueiredo, B. Achiaga, R. Barea, D. Pérez-Coll, A. Morelos-Gómez, M. Terrones, M.I. Osendi, M. Belmonte, P. Miranzo, Electrically functional 3D-architectured graphene/SiC composites, Carbon 100 (2016) 318–328. https://doi.org/10.1016/j.carbon.2015.12.103

[17] Z. Guo, L. An, S. Khuje, A. Chivate, J. Li, Y. Wu, Y. Hu, J. Armstrong, S. Ren, C. Zhou, 3D-printed electrically conductive silicon carbide, Addit. Manuf. 59 (2022) 103109. https://doi.org/10.1016/j.addma.2022.103109

[18] H. Liu, Y. Li, R. Tang, Y. Li, 3D Printing of Polymer-Derived Graphene/SiCp/SiC Composite by Direct Ink Writing, Crystals 15 (2024) 11. https://doi.org/10.3390/cryst15010011

[19] L. Moreno-Sanabria, C. Ramírez, M.I. Osendi, M. Belmonte, P. Miranzo, Enhanced Thermal and Mechanical Properties of 3D Printed Highly Porous Structures Based on γ-Al₂O₃ by Adding Graphene Nanoplatelets, Adv. Mater. Technol. 7 (2022) 2101455. https://doi.org/10.1002/admt.202101455

[20] L. Moreno-Sanabria, T. Uhlířová, W. Pabst, M. Koller, H. Seiner, M.I. Osendi, M. Belmonte, P. Miranzo, Effective Young’s modulus of highly porous 3D printed mono-material and coaxial structures, J. Eur. Ceram. Soc. 44 (2024) 116771. https://doi.org/10.1016/j.jeurceramsoc.2024.116771

[21] L. Moreno-Sanabria, I. Díaz-Herrezuelo, M.I. Osendi, M. Belmonte, P. Miranzo, Coaxially 3D-printed ceramic scaffolds for thermal energy storage applications, J. Eur. Ceram. Soc. 45 (2025) 117531. https://doi.org/10.1016/j.jeurceramsoc.2025.117531

[22] D. Budáč, V. Miloš, M. Carda, M. Paidar, K. Bouzek, J. Fuhrmann, A Monte Carlo Approach for Simulating Electrical Conductivity in Highly Porous Ceramic Composites: Impact of Internal Structure, ACS Appl. Mater. Interfaces 16 (2024) 62292–62300. https://doi.org/10.1021/acsami.4c08287

[23] Y. Wu, C. An, Y. Guo, 3D Printed Graphene and Graphene/Polymer Composites for Multifunctional Applications, Materials 16 (2023) 5681. https://doi.org/10.3390/ma16165681

[24] H. R, M.I. Shajahan, R. Čep, S. Salunkhe, A.P. Murali, G. Sharad, H.M.A. Hussein, E. Abouel Nasr, Electrical conductivity analysis of extrusion-based 3D-printed graphene, Front. Mater. 11 (2024) 1328347. https://doi.org/10.3389/fmats.2024.1328347

[25] J. Han, I.E.A. Elfaki, L. Weston, C. Chen, D.A. Klosterman, L. Cao, Development of SiC Nanocomposites Using Direct Ink Writing Process, Adv. Eng. Mater. 27 (2025) e202501688. https://doi.org/10.1002/adem.202501688

[26] H. Han, Q. Hu, X. Yang, Additive manufacturing of fiber-reinforced silicon carbide ceramic matrix composites: process optimization and performance control, Ceram. Int. 51 (2025) 45205–45224. https://doi.org/10.1016/j.ceramint.2025.07.239

[27] K.R. Cox, T.D. Marconie, R.A.S. Barger, K.M. Motwani, J.P. Youngblood, R.W. Trice, Slurry material extrusion of chopped carbon fiber reinforced silicon carbide ceramic matrix composites (CMCs), Int. J. Appl. Ceram. Technol. 22 (2025) e14915. https://doi.org/10.1111/ijac.14915

[28] Z. Xu, J. Zhao, M. Liu, Z. Liu, X. Cheng, J. Chang, X. Yang, B. Li, B. Liu, R. Liu, Enhanced strength and toughness of SiC/C composite ceramics via SiC@graphene core–shell nanoparticles, J. Am. Ceram. Soc. 108 (2025) e20151. https://doi.org/10.1111/jace.20151

[29] H. Xu, Y. Liu, Z. Chen, K. Wang, Microstructure and mechanical properties of carbon nanotube-reinforced silicon carbide composites fabricated by direct ink writing and reaction bonding, J. Mater. Sci. 177 (2026) 289–302. https://doi.org/10.1007/s10853-026-12431-6

[30] V. Bishop, S.C. Mathur, N. Nguyen, B. Sharma, M. Drouin, B. Li, C. Park, W. Wei, A review of direct ink writing of polymer derived ceramics, Virtual Phys. Prototyp. 20 (2025) 2499938. https://doi.org/10.1080/17452759.2025.2499938