1. Introduction

Silicon carbide (SiC) ceramics are among the most versatile structural materials available today, owing to their exceptional hardness, high-temperature stability, chemical inertness, and favorable thermal conductivity [1,2]. These attributes have made SiC ceramics indispensable in aerospace propulsion, advanced electronics, and energy-conversion systems [3]. However, the intrinsic electrical conductivity of pure SiC (∼10⁻⁶–10⁻² S·m⁻¹) is too low for applications such as Joule heating elements, electromagnetic interference (EMI) shielding, electrostatic discharge (ESD) substrates, and electrochemical electrodes [4,5]. Overcoming this limitation without sacrificing the mechanical and thermal advantages of the SiC matrix is therefore a key challenge in current ceramic engineering [6].

Since its isolation in 2004 [29], graphene has attracted enormous attention as a multifunctional filler for ceramic matrices due to its outstanding electrical conductivity (∼10⁶ S·m⁻¹), high specific surface area (2630 m²·g⁻¹), and remarkable mechanical strength (∼130 GPa intrinsic strength) [7,14,20,21]. In SiC-based composites, graphene nanoplatelets (GNPs) form a percolative conductive network at relatively low filler loadings, boosting room-temperature conductivity by up to three to four orders of magnitude compared with the undoped matrix [12,31]. Moreover, the two-dimensional morphology of GNPs activates crack-deflection and crack-bridging toughening mechanisms that simultaneously improve fracture toughness [7,22]. Recent comprehensive reviews have summarized the processing routes, microstructural design, and multifunctional properties of graphene/SiC composite ceramics [14,20,21,35].

Conventionally, dense graphene/SiC composites are produced by hot-pressing (HP) or spark plasma sintering (SPS) at temperatures above 1800 °C and pressures of 30–50 MPa [12,31]. While these techniques yield high relative densities (≥98%), they are inherently limited to simple bulk geometries—plates, discs, or cylinders—and the uniaxial pressure applied during sintering induces strong preferential alignment of GNPs perpendicular to the pressing axis, resulting in pronounced anisotropy of both electrical and thermal conductivity [31,35]. Furthermore, high sintering temperatures can degrade graphene through thermal reduction or reaction with the SiC matrix, diminishing the intended property enhancements [7,14]. These constraints motivate the exploration of additive manufacturing (AM) routes that can create three-dimensional architectured composites with controlled porosity and topology at substantially lower processing temperatures [1,2].

Among the various AM techniques applicable to ceramics, direct ink writing (DIW)—also termed robocasting—has emerged as a particularly attractive approach [2,5,30]. In DIW, a viscoelastic ceramic-loaded ink is extruded through a fine nozzle in a computer-controlled pattern, enabling layer-by-layer construction of complex three-dimensional lattice structures with programmable pore size, strut diameter, and stacking architecture [18,19,34]. The technique operates at ambient temperature and pressure, which preserves the structural integrity of carbon fillers such as graphene and carbon nanotubes [10,16,17]. Significant progress has been made in ceramic DIW ink formulation, with recent meta-analyses and reviews systematically mapping the relationships among solid loading, rheological parameters, and printability [13,18,19,28].

The pioneering work of Román-Manso et al. [33] demonstrated that graphene/SiC scaffold structures fabricated by DIW and partially sintered at 1500“1800 °C can reach effective conductivities on the order of 611 S·m⁻¹, a value governed not only by the graphene content but also by the lattice architecture. Subsequent studies by Moyano et al. [3,9,37] explored multiscale porosity design, recycling of robocast scraps, and the influence of partial sintering on the mechanical and electrical performance of these composites. Moreno-Sanabria et al. [11,24,27] extended the DIW approach to coaxial multi-material scaffolds and investigated the effective mechanical properties of highly porous 3D-printed structures using both experiment and finite element modelling (FEM). An et al. [8] reported 3D-printed SiC lattices with conductivities exceeding 1000 S·m⁻¹ through polymer-derived ceramic processing, while Xiao et al. [26] achieved 670 S·m⁻¹ in DIW graphene/SiCp/SiC composites via a similar route.

A critical yet under-explored variable in these studies is the role of lattice topology—i.e., the geometric arrangement of filaments within the structure—in determining the effective electrical transport properties of DIW ceramics. Different stacking patterns (e.g., orthogonal grid, rotated honeycomb, offset scaffold) produce fundamentally different interlayer contact areas, filament alignment relative to the applied electric field, and current density distributions [6,33]. Tabares et al. [6] showed that lattice topology strongly influences the mechanical response of DIW structures, and analogous architecture-dependent effects on electrical properties have been observed for 3D-printed graphene-based composites [15,23,25]. However, a systematic comparison of multiple lattice topologies under identical material and printing conditions, with explicit quantification of the topology–conductivity relationship, remains absent in the literature.

Finite element modelling (FEM) provides a powerful complementary approach for understanding these architecture–property relationships. By solving Maxwell’s equations (or their DC-conduction simplification) on a digitised representation of the actual lattice geometry, FEM can predict effective conductivity, map local current-density (J-field) distributions, and identify bottleneck regions that govern macroscopic transport [27,36]. Ramírez et al. [36] proposed an analytical/numerical model for the conductivity of bulk graphene/SiC nanocomposites, and Moreno-Sanabria et al. [27] recently demonstrated the use of FEM to explain the thermal behaviour of coaxially 3D-printed ceramic scaffolds. Despite these advances, no study has applied full three-dimensional FEM simulation—especially DC conduction analysis using commercial solvers such as ANSYS Maxwell 3D—to compare the electrical performance of different DIW lattice architectures of graphene/SiC composites, correlating the simulation output with experimentally measured conductivities.

The present study addresses this gap by combining ANSYS Maxwell 3D DC conduction FEM simulation with four-probe experimental measurements to systematically investigate the effective electrical conductivity of three representative lattice architectures—Grid, Honeycomb, and Scaffold—fabricated from the same graphene/SiC composite ink by DIW. Specifically, the work aims to answer three research questions: (i) How does lattice architecture determine the effective conductivity σeff when the solid-phase volume fraction is held constant? (ii) What are the respective roles of the interlayer contact area (Aint) and filament–field alignment angle in governing the current transport? (iii) How do the local J-field distributions differ among the three architectures, and what functional trade-offs (uniformity vs. peak conductivity) do they imply?

The remainder of this paper is organised as follows. Section 2 describes the experimental procedures, including ink preparation, DIW printing parameters, sintering protocol, and four-probe electrical characterisation, as well as the FEM simulation methodology (solver settings, boundary conditions, mesh convergence, and post-processing). Section 3 presents the simulation and experimental results for the three lattice architectures, with a detailed analysis of conductivity, resistance, and current-density fields. Section 4 discusses the key findings in the context of the existing literature, and Section 5 summarises the conclusions and outlines future work.

References

[1] Y. Lakhdar, C. Tuck, J. Binner, A. Terry, R. Goodridge, Additive manufacturing of advanced ceramic materials, Prog. Mater. Sci. 116 (2021) 100736.

[2] A. Shahzad, I. Lazoglu, Direct ink writing (DIW) of structural and functional ceramics: recent achievements and future challenges, Compos. Part B: Eng. 225 (2021) 109249.

[3] J.J. Moyano, E. Camposilvan, M. Belmonte, M.I. Osendi, P. Miranzo, Strong and light cellular silicon carbide/graphene composites prepared by direct ink writing and partial sintering, Carbon 177 (2021) 289–302.

[4] C. Ramírez, M. Belmonte, P. Miranzo, M.I. Osendi, Applications of ceramic/graphene composites and hybrids, Materials 14(8) (2021) 2071.

[5] M.L. Sesso, S.S.L. Chan, G.V. Franks, Direct ink writing of hierarchically porous alumina using emulsified ceramic inks, J. Am. Ceram. Soc. 104(10) (2021) 4977–4990.

[6] E. Tabares, B. Justa, Y. Torres, M. Belmonte, Mechanical characterisation of lattice structures fabricated by direct ink writing, Ceram. Int. 47(12) (2021) 17456–17465.

[7] W. Zhao, C. Ma, H. Wang, L. Chen, Z. Huang, Effects of graphene content on the microstructure and properties of SiC ceramics, Ceram. Int. 47(24) (2021) 33941–33955.

[8] L. An, B. Liang, Z. Guo, J. Wang, C. Li, Y. Huang, Y. Hu, Z. Li, J.N. Armstrong, C. Zhou, R. Wu, 3D-printed electrically conductive silicon carbide, Addit. Manuf. 58 (2022) 103041.

[9] J.J. Moyano, A. Fernández, M. Belmonte, M.I. Osendi, P. Miranzo, Multiscale porosity by direct ink writing and pressureless partial sintering of graphene/SiC composites, Open Ceram. 8 (2022) 100192.

[10] A.J. Allen, I. Levin, S.E. Witt, Research, standards, and data needs for industrialization of ceramic direct ink writing, Int. J. Ceram. Eng. Sci. 4(5) (2022) 330–339.

[11] L. Moreno-Sanabria, M. Belmonte, M.I. Osendi, P. Miranzo, Enhanced thermal and mechanical properties of 3D printed highly porous structures based on γ-Al₂O₃ by adding graphene nanoplatelets, Adv. Mater. Technol. 7(8) (2022) 2101455.

[12] R. Sedlák, A. Kovalcíková, C. Balázsi, J. Dusza, SiC-based ceramics with remarkable electrical conductivity prepared by ultrafast high-temperature sintering, Ceram. Int. 49(11) (2023) 18091–18098.

[13] A. Shahzad, A. Mahajani, I. Lazoglu, An overview of ceramic 3D printing: the path towards industrialization, J. Eur. Ceram. Soc. 43(16) (2023) 7482–7510.

[14] J. Chen, B. Liu, G. Zhang, H. Li, W. Zhang, Preparation and properties of graphene/SiC composite ceramics: a review, J. Mater. Sci. 58(4) (2023) 1625–1651.

[15] B. Fan, H. Guo, J. Shi, C. Shi, Y. Jia, H. Wang, D. Chen, Y. Yang, H. Lu, H. Xu, R. Zhang, 3D printed graphene and graphene/polymer composites for multifunctional applications, Polymers 15(17) (2023) 3622.

[16] I.S. Elizarova, L. Vandeperre, E. Saiz, Conformable green bodies: plastic forming of robocasted advanced ceramics, J. Eur. Ceram. Soc. 43(6) (2023) 2832–2841.

[17] Y. Zhao, J. Zhu, W. He, Y. Liu, X. Sang, R. Liu, 3D printing of unsupported multi-scale and large-span ceramic via near-infrared assisted direct ink writing, Nat. Commun. 14 (2023) 2381.

[18] Y. Lakhdar, L. Biasetto, P. Colombo, E. García-Tuñón, Ink formulation in direct ink writing of ceramics: a meta-analysis, J. Eur. Ceram. Soc. 44(14) (2024) 116665.

[19] A. Dey, M.B. Rashid, F. Wang, S. Mahmud, J. Jin, Direct ink writing 3D printing of ceramics: a review, Ceram. Int. 50(24) (2024) 55027–55064.

[20] W. Zou, S. Li, G. Wang, Z. Zhang, Y. Zhou, Graphene reinforced silicon carbide ceramic composites: processing, properties and applications, Ceram. Int. 50(17) (2024) 29866–29876.

[21] M. Singh, V. Sharma, B. Singh, Graphene reinforced SiC ceramic composites using powder metallurgy route: a short review, Silicon 16(9) (2024) 3617–3635.

[22] A. Almansoori, K.O. Mustapha, A. Alshammari, M. Alkahtani, Advances, challenges, and applications of graphene and carbon nanotube-reinforced engineering ceramics, Nanomaterials 14(23) (2024) 1899.

[23] R. Harikrishnan, M.I. Shajahan, R. Čep, S. Salunkhe, A.P. Murali, G. Sharad, H.M.A. Hussein, E. Abouel Nasr, Electrical conductivity analysis of extrusion-based 3D-printed graphene, Front. Mater. 11 (2024) 1328347.

[24] L. Moreno-Sanabria, T. Uhlířová, W. Pabst, M. Koller, H. Seiner, M.I. Osendi, M. Belmonte, P. Miranzo, Effective Young’s modulus of highly porous 3D printed mono-material and coaxial structures, J. Eur. Ceram. Soc. 44(15) (2024) 116771.

[25] E. Choi, S. Kim, S. Lee, Mechanical and electrical properties of 3D-printed highly conductive reduced graphene oxide/polylactic acid composite, Adv. Eng. Mater. 26(5) (2024) 2301732.

[26] S. Xiao, H. Liu, Z. Ren, J. Lin, J. Fan, 3D printing of polymer-derived graphene/SiCp/SiC composite by direct ink writing, Crystals 15(1) (2025) 11.

[27] L. Moreno-Sanabria, I. Díaz-Herrezuelo, M.I. Osendi, M. Belmonte, P. Miranzo, Coaxially 3D-printed ceramic scaffolds for thermal energy storage applications, J. Eur. Ceram. Soc. 45(14) (2025) 117531.

[28] V. Bishop, S.C. Mathur, N. Nguyen, B. Sharma, M. Drouin, B. Li, C. Park, W. Wei, A review of direct ink writing of polymer derived ceramics, Virtual Phys. Prototyp. 20(1) (2025) 2499938.

[29] K.S. Novoselov, A.K. Geim, S.V. Morozov, D. Jiang, Y. Zhang, S.V. Dubonos, I.V. Grigorieva, A.A. Firsov, Electric field effect in atomically thin carbon films, Science 306(5696) (2004) 666–669.

[30] J.A. Lewis, Direct ink writing of 3D functional materials, Adv. Funct. Mater. 16(17) (2006) 2193–2204.

[31] B. Román-Manso, F.M. Figueiredo, B. Achiaga, M. Belmonte, M.I. Osendi, P. Miranzo, Enhanced electrical conductivity of silicon carbide ceramics by addition of graphene nanoplatelets, J. Eur. Ceram. Soc. 35(10) (2015) 2723–2731.

[32] N.P. Padture, Advanced structural ceramics in aerospace propulsion, Nat. Mater. 15(8) (2016) 804–809.

[33] B. Román-Manso, F.M. Figueiredo, B. Achiaga, R. Barea, D. Perez-Coll, A. Morelos-Gómez, M. Terrones, M.I. Osendi, M. Belmonte, P. Miranzo, Electrically functional 3D-architectured graphene/SiC composites, Carbon 100 (2016) 318–328.

[34] E. Feilden, E. García-Tuñón Blanca, F. Giuliani, E. Saiz, L. Vandeperre, Robocasting of structural ceramic parts with hydrogel inks, J. Eur. Ceram. Soc. 36(10) (2016) 2525–2533.

[35] P. Miranzo, M. Belmonte, M.I. Osendi, From bulk to cellular structures: a review on ceramic/graphene filler composites, J. Eur. Ceram. Soc. 37(12) (2017) 3649–3671.

[36] C. Ramírez, M.I. Osendi, P. Miranzo, M. Belmonte, F.M. Figueiredo, Modelling the electrical conductivity of graphene/SiC-ceramic nanocomposites, Ceram. Int. 43(15) (2017) 11930–11938.

[37] J.J. Moyano, M. Belmonte, P. Miranzo, M.I. Osendi, Recycling of graphene and silicon carbide from ground scraps of robocast structures for use in new ceramic inks, Ceram. Int. 45(15) (2019) 18797–18805.