4. Discussion

4.1. FEM–experiment correlation

Both FEM and experiment yield an identical architecture-dependent ranking of effective electrical conductivity: σeff,Grid < σeff,Scaffold < σeff,Honeycomb (Tables 1 and 2). The FEM-predicted values are 10.780, 12.109, and 12.943 S/m, while the measured values are 6.240 ± 0.095, 9.916 ± 0.314, and 10.869 ± 0.250 S/m, respectively. The preservation of this ranking confirms that the differences in electrical transport originate from the lattice topology and interlayer connectivity, not from stochastic fabrication variability.

The experimental σeff values are systematically lower than the FEM predictions by a factor of 1.19–1.73. This offset is consistent with dissipation mechanisms absent in the idealised FEM model: (i) finite interlayer contact resistance at incompletely sintered filament–filament junctions, (ii) residual porosity and local heterogeneity in graphene–SiC phase distribution, and (iii) dimensional deviations from the nominal CAD geometry caused by drying shrinkage and sintering densification. The discrepancy is architecture-dependent: σeff,FEM/σeff,exp = 1.73 for Grid, 1.22 for Scaffold, and 1.19 for Honeycomb. The larger offset for Grid is attributed to the high density of in-plane turning points in the meander toolpath, where abrupt filament direction changes are prone to local over- or under-extrusion during DIW, amplifying geometric deviations in the sintered specimen. The Scaffold and Honeycomb toolpaths contain longer straight-run segments with fewer turns, yielding better geometric fidelity and smaller FEM–experiment offsets.

4.2. Solid volume, interlayer contact area, and topology effects

The three models were designed with comparable solid volumes within the same specimen envelope: VGrid = 467.206 mm³, VScaffold = VHoneycomb = 443.748 mm³. The Grid contains 5.3% more conductive material than the Scaffold and Honeycomb. For a homogeneous conductor (R = L/σA), a larger conductive volume at fixed dimensions should reduce resistance. However, the Grid exhibits the highest R (FEM: 15.385 Ω; exp: 34.983 Ω) and the lowest σeff. If volume were the dominant factor, the Grid should show σeff ∼5% higher than the Scaffold; instead, σeff,Grid is 11% lower in FEM and 37% lower experimentally. This quantitative deficit demonstrates that the structural architecture—specifically, current-path tortuosity and interlayer contact geometry—exerts a stronger influence on σeff than moderate variations in material loading.

The interlayer contact area Aint at individual filament crossings quantifies the geometric bottleneck for through-thickness current transfer. For Scaffold and Grid (θc = 90°), Aint = 0.0844 mm². For Honeycomb (θ = 60°), Aint = 0.3632 mm²—a factor of 4.3× larger. The constriction resistance at a single contact scales as Rconstr ∝ 1/(2σa), where a is the characteristic contact dimension (Aint ∝ a²). A 4.3× increase in Aint raises a by √4.3 ≈ 2.07, reducing Rconstr per crossing by approximately a factor of 2. Summed over all serial and parallel interlayer junctions in the 12-layer stack, this reduction in local constriction resistance produces the lowest bulk R for the Honeycomb topology.

The Scaffold and Grid share identical Aint = 0.0844 mm², yet Scaffold exhibits higher σeff (12.109 vs. 10.780 S/m in FEM; 9.916 vs. 6.240 S/m experimentally). This difference cannot originate from the contact area and is governed by the current-path organisation. In the Scaffold 0°/90° cross-ply layup, one filament set spans the full specimen length parallel to E, providing a low-resistance conduction highway; the orthogonal set serves as interlayer bridges. In the Grid, every filament segment is inclined at an oblique angle to E, increasing the effective electrical path length (Leff = L/cosα > L) and cumulative resistance. The Grid’s meander toolpath also introduces a high density of turning-point constrictions that add further resistive loss.

Beyond Aint per crossing, the total interlayer contact area per interface, Atotal = Ncross × Aint, governs cumulative constriction resistance. In the Scaffold (0°/90°), every filament crosses every filament of the adjacent layer, maximising Ncross for a given pitch hp. The Grid distributes crossings along diamond-cell boundaries, leaving node-free voids at cell interiors. The Honeycomb generates fewer crossings per interface than the Scaffold but compensates through the 4.3× larger Aint per crossing, yielding the highest Atotal and hence the lowest cumulative constriction resistance. Normalising σeff by solid volume confirms the material-efficiency hierarchy: σeff/V = 0.0292 (Honeycomb), 0.0273 (Scaffold), and 0.0231 S·m−1·mm−3 (Grid)—the Honeycomb achieves 26% higher conductivity per unit material than the Grid.

4.3. Comparative J-vector field analysis and bottleneck formation

Grid. The J-vector field maps (Fig. 8a,b) show that both track sets exhibit comparably dense vector filling at the upper range of the logarithmic |J| scale. The magnified insets reveal only localised reductions in vector density at interlayer contact zones. This uniform distribution arises because no filament segment is oriented perpendicular to E: every segment carries a non-zero current component along the field direction. The full-lattice map (Fig. 8c) retains this dense, spatially continuous character throughout the grid domain, with constrictions confined to grid nodes and interlayer contacts. The A–A cross-section confirms that even at the interlayer interfaces, the vector concentration remains moderate. Among the three architectures, the Grid exhibits the most uniform J-field. Despite the lowest σeff, this characteristic represents a high potential for applications demanding homogeneous current distribution (sensors, uniform heating elements) rather than minimum resistance, since the current density is evenly utilised across the entire conductive volume.

Scaffold. The Scaffold J-field (Fig. 10) exhibits a pronounced bimodal pattern. Tracks parallel to E (Fig. 10a) display dense, rectilinear vector filling with |J| concentrated at the upper logarithmic scale—the current flows efficiently along the full filament length without redirection. Tracks perpendicular to E (Fig. 10b) show markedly more heterogeneous |J|: extended yellow–green regions (low |J|) appear between contact nodes, and locally elevated |J| is concentrated at junction regions where current transfers between layers. The physical interpretation is direct: in the perpendicular filaments, current enters and exits exclusively through Aint = 0.0844 mm² contact zones and traverses only a short transverse segment before transferring to the next parallel filament. Filament sections between consecutive contact points carry little current because they are not aligned with E and are in series with high-constriction-resistance junctions. The A–A cross-section (Fig. 10c) confirms the rarefied J-field in perpendicular layers compared to longitudinal ones. Despite this interlayer rarefaction, the parallel tracks provide an efficient conduction highway that enables IScaffold = 0.365 A, which is 12% higher than IGrid = 0.325 A under the same 5 V bias.

Honeycomb. Track set 1 (longitudinal, Fig. 9a) shows high vector filling and quasi-uniform |J| along the conducting tracks, with localised reductions at zig-zag apices where the filament changes direction by the turning angle α. Track set 2 (at 65° to E, Fig. 9b) is considerably more heterogeneous: extended yellow–green zones are interspersed with orange-level segments, and locally elevated |J| zones coincide with interlayer junctions and geometrically constrained conducting transitions. The magnified insets confirm pronounced local changes in vector density and orientation at junction and turn segments. In the full 12-layer lattice (Fig. 9c), the most severe |J| variations are concentrated at interlayer intersections, where the current must pass through the contact zones. Despite Aint = 0.3632 mm² being 4.3× larger than in the other topologies, each zig-zag turn introduces a geometric constriction that forces local |J| peaks flanked by rarefied regions. These bottleneck features at interlayer junctions are characteristic of the honeycomb geometry, confirmed by both magnified views and the A–A cross-section.

A clear trade-off emerges from this comparison: the J-field uniformity decreases in the order Grid > Scaffold (parallel tracks) > Honeycomb, while σeff increases in the reverse order. The Grid minimises tortuosity and distributes current most evenly among all filament segments but pays a penalty in elevated path length and cumulative resistance. The Honeycomb minimises constriction resistance through enlarged Aint but introduces local bottlenecks at zig-zag turns that produce a wider spread of local |J| values. This inverse relationship reflects a fundamental constraint in lattice-based conductors: maximising interlayer contact area to reduce bulk resistance inherently requires oblique filament crossings that disrupt J-field uniformity. The choice of architecture therefore depends on the target application—minimum resistance versus uniform current distribution.

5. Conclusions

Three topology-controlled 3D graphene–SiC lattice architectures (Grid, Scaffold, Honeycomb) were fabricated by DIW and sintered at 1300 °C. Effective electrical conductivities were evaluated by steady-state DC FEM simulations and four-probe DC measurements. The principal findings are:

(1) FEM and experiment yield the same ranking: σeff,Grid (10.780 / 6.240 S/m) < σeff,Scaffold (12.109 / 9.916 S/m) < σeff,Honeycomb (12.943 / 10.869 S/m), confirming that the topology governs the electrical response.

(2) The interlayer contact area Aint is the primary structural determinant. The Honeycomb’s oblique crossings (θ = 60°) produce Aint = 0.3632 mm², 4.3× larger than the 90° crossings (0.0844 mm²) in Scaffold and Grid, directly reducing constriction resistance and yielding the highest σeff.

(3) At identical Aint, the Scaffold achieves 12% (FEM) to 59% (experiment) higher σeff than the Grid despite 5.3% less solid material, demonstrating that current-path alignment with the field direction dominates over material volume.

(4) J-vector field analysis reveals an inverse relationship between σeff and J-field uniformity. The Grid exhibits the most uniform |J| distribution due to all filaments carrying a field-parallel current component. The Honeycomb, despite the highest σeff, shows the most heterogeneous local |J| with bottlenecks at zig-zag turns and interlayer junctions.

(5) The FEM–experiment offset (factor 1.19–1.73) is attributed to interlayer contact resistance, residual porosity, and sintering-induced dimensional deviations. The Grid shows the largest offset (1.73), consistent with its sensitivity to geometric imperfections at the numerous in-plane turning points.

(6) The lattice architecture is the dominant design lever for tailoring electrical conductivity in DIW-printed graphene–SiC lattices. Aint and filament–field alignment are the two independent structural parameters that can be optimised to achieve either maximum conductivity (Honeycomb) or maximum J-field uniformity (Grid).